## Slide 1
©copyright by HarvardDental
Harvard InterLock ONE
The truly Universal adhesive

## Slide 2
Interlock ONE – The Great Performer
interceptor:
Thread remains clean
Bonding cures completely during demonstration
modern snap-off ampoules available
©copyright by HarvardDental
Adhesives
Harvard UltraFill.

## Slide 3
Benefits of Universal Bonding Agents
Universal Bonding Agents work in every case:
On un-etched dentin
On pre-etched dentin
On un-etched enamel
On pre-etched enamel
On dry surfaces
On wet surfaces
Together with dual curing restoratives
Together with self curing restoratives (mixed with an activator)
©copyright by HarvardDental
Adhesives
Harvard InterLock ONE.

## Slide 4
Benefits of Universal Bonding Agents
Only 1 bonding agent at the chair for all „light curing“ indications
  Direct composites
  Veneer cementation
  Inlay/Onlay cementation
  Adhesive porcelain crown cementation
  Core Build-up procedures
    With self cure activator it becomes self cure, for:
      Adhesive metal crown cementation
      Post cementation in root canals
©copyright by HarvardDental
Adhesives
Harvard InterLock ONE.

## Slide 5
Benefits of Universal Bonding Agents
Reduced postoperative sensitivity under self-etch conditions
  Very important for crown cementation
„Over-Etching“ is avoided. No total-etch risk on dentin Typical problem in selective etch procedures
Selective Etch performance in high risk areas
  Cementum/enamel junction; approximal axial walls
Overcomes the „how wet is wet“-problem
  Different Air-gun pressures?, how long drying time?
  Re-wetting of the hybrid layer on overdried dentin
©copyright by HarvardDental
Adhesives
Harvard InterLock ONE.

## Slide 6
Drop-Control
©copyright by HarvardDental
Adhesives
Harvard InterLock ONE.
Safe and controlled drop shapes
Constant drop volume of 10-20 microliter – exact amount that a brush can take on
Interceptor in the dripper: liquid runs back into the bottle
Always clean label information, clean bottle
Equalling of the drop size with 2- or more component materials
260 drops = 260 applications

## Slide 7
Shearbond strength on Dentin + Enamel
After Thermocycling :
©copyright by HarvardDental
7
Adhesives
Harvard InterLock One.
Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
= stress test simulation of wear for ca.1 year
Notes: Self etching tissues with bonding agent, light cured composite

## Slide 8
Chart: 
| Interlock ONE | Prime & Bond Active | Scotchbond Universal | Optibond All-In-One
 | 32 | 13.2 | 12.8 | 14.4
 | 20.8 | 18.9 | 13.6 | 23.5
Dentin
Enamel
Dentin
Dentin
Dentin
Enamel
Enamel
Enamel
Self-etch shearbond strength
Dentin & enamel after thermocycling, Adhesive light cured & composite self cured
©copyright by HarvardDental
8
Adhesives
Harvard InterLock One.
InterLock ONE
Dentsply
Prime&Bond Active
3MEspe
Scotchbond Universal
KaVoKerr
Optibond All-In-One
= stress test simulation of wear for ca.1 year - Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
Self-Etch with composite self-cured
Notes: Self etching tissues with bonding agent, self cured composite; for instance core build up material

## Slide 9
Chart: 
| Self etch & LC | Self etch & self cure | Total etch & LC | Total etch & self cure
 | 35 | 32 | 23.8 | 9
 | 19.1 | 20.8 | 29.3 | 30.8
Dentin
Enamel
Dentin
Dentin
Dentin
Enamel
Enamel
Enamel
©copyright by HarvardDental
9
Adhesives
Harvard InterLock One.
InterLock ONE
Dentsply
Prime&Bond Active
3MEspe
Scotchbond Universal
KaVoKerr
Optibond All-In-One
= stress test simulation of wear for ca.1 year - Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
Selective etch on enamel
Dentin & enamel after thermocycling, Adhesive: Light cured
Etching: Total Etch or self etch; Composite: Light cured or self cured
Notes: Self etching tissues with bonding agent, self cured composite; for instance core build up material

## Slide 10
Chart: 
| Interlock ONE | Prime & Bond Active | Scotchbond Universal | Optibond All-In-One
 | 35 | 22.9 | 20.1 | 10.1
 | 19.1 | 6.2 | 7.7 | 18.4
Dentin
Enamel
Dentin
Dentin
Dentin
Enamel
Enamel
SELF-etch shearbond strength
Dentin & enamel after thermocycling, Adhesive light cured & composite light cured
©copyright by HarvardDental
10
Adhesives
Harvard InterLock One.
InterLock ONE
Dentsply
Prime&Bond Active
3MEspe
Scotchbond Universal
KaVoKerr
Optibond All-In-One
Enamel
= stress test simulation of wear for ca.1 year - Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
Notes: Total etching tissues with phosphoric acid, conditioning with bonding agent, light cured composite

## Slide 11
Chart: 
| Interlock ONE | Prime & Bond Active | Scotchbond Universal | Optibond All-In-One
 | 23.8 | 25.2 | 14.2 | 6.3
 | 29.3 | 32.6 | 24.5 | 27.3
Dentin
Enamel
Dentin
Dentin
Dentin
Enamel
Enamel
Enamel
Total-etch shearbond strength
Dentin & enamel after thermocycling, Adhesive light cured & composite light cured
©copyright by HarvardDental
11
Adhesives
Harvard InterLock One.
InterLock ONE
Total Etch with composite light cured
Dentsply
Prime&Bond Active
3MEspe
Scotchbond Universal
KaVoKerr
Optibond All-In-One
Enamel
= stress test simulation of wear for ca.1 year - Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
Notes: Total etching tissues with phosphoric acid, conditioning with bonding agent, light cured composite

## Slide 12
Chart: 
| Interlock ONE | Prime & Bond Active | Scotchbond Universal | Optibond All-In-One
 | 9 | 9.7 | 11.4 | 0
 | 30.8 | 23.5 | 23.5 | 21.2
Dentin
Enamel
Dentin
Dentin
Dentin
Enamel
Enamel
Enamel
Total-etch shearbond strength
Dentin & enamel after thermocycling, Adhesive light cured & composite self cured
©copyright by HarvardDental
12
Adhesives
Harvard InterLock One.
InterLock ONE
Dentsply
Prime&Bond Active
3MEspe
Scotchbond Universal
KaVoKerr
Optibond All-In-One
Total Etch with composite self cured
= stress test simulation of wear for ca.1 year - Subjected to 2,000 thermocycles between 5° and 55° C with a dwell time of 30 s.
Notes: Total etching tissues with phosphoric acid, conditioning with bonding agent, self cured composite; root canal post bonding, metal crown cementation

## Slide 13
really Universal Adhesive
allows for bonding of ceramic, zirconia metal crowns with composite cements
very high bond strength after stress test long-term stability
extremely good marginal behaviour
contains MDP
pH-value: 2,5
solving agent: Ethanol (pleasant smell)
always constant drop size
content: 260 drops= good calculation in the dental office
– State of the art
MDP
©copyright by HarvardDental
Adhesives
Harvard InterLock One.
Notes: MDP = Methacryloyloxy Decyl (Dihydrogen) Phosphat

## Slide 14
HARVARD InterLock ONE
One of the best bonding agents on the market
Special Combi Kits with PremiumFill+ and UltraFill
With Light
Success is a 2-bladed golden sword!
Mae West
HARVARD InterLock Self-Cure Activator
For self-curing cases:
InterLock One + Self Cure Activator
For all indications
For root post cementations
For metal crown fixation
Without light
&
Adhesives